Kesfloor DPM2

SURFACE DAMP PROOF MEMBRANE

INTRODUCTION

Kesfloor DPM2 is a two part epoxy moisture vapour suppressant and surface damp proof membrane.

Tested to European Standard pr EN 104.. (16)

USE

Kesfloor DPM2 is used to form a surface damp proof membrane and moisture vapour suppressant to concrete and sand/ cement floors.

ADVANTAGES

*Provides a surface damp proof membrane.

*Ideal for suppressing residual moisture in concrete and sand / cement.

*Allows early laying of floor covering.

*Kesfloor DPM2 provides a sandwich damp proof membrane and bonding agent for quick cure screeds.

*Can accommodate RH’s up to 97%.

*Cost effective.

*Easy to apply.

*Two colour coat system provides a visual control on application.

SYSTEM / COLOURS

Primer Coat:  	Red.

Top Coat:	Green.

On application the two colours provide a visual control in ensuring uniform coverage.

Can be supplied clear.

COMPOSITION

Kesfloor DPM2 is a two part solvent free flexibilised epoxy, containing wetting agents, penetrants,

flow agents and defoamers to maximise penetration and adhesion and to minimise pinholes.

Primer:

Part A: Low viscosity, Red in colour, packed in a larger container to allow mixing.

Part B: Low viscosity hardener, clear colour.

Top Coat:

Part A: Low viscosity, Green in colour, packed in a larger container to allow mixing.

Part B: Low viscosity hardener, clear colour.

PACKAGING

Packed in 5 litre units.

MIXING

Add contents of part B to part A and mix thoroughly. Failure to mix thoroughly could result in a poor or non-cure material.

APPLICATION

Kesfloor DPM2 can be applied by brush, roller or airless spray.

COVERAGE RATE

Primer:

To obtain the desired film thickness the coverage rate will depend on the porosity of the concrete.

Top Coat:

To obtain the desired film thickness the topcoat should be applied at 5m2 per litre.

STORAGE

Store in sealed containers between 5c and 30c

CLEANING

A suitable cleaning solvent should be used for cleaning tools etc.

HEALTH AND SAFETY

See separate Health and Safety Data Sheet.

WARRANTY DISCLAIMER

The technical data herein has been compiled for your help and guidance and is based upon our experience. As we have no control over the use to which our information is put, no warranty, expressed or implied is intended or given and we cannot be held responsible for coverage, performance or any damages incurred.

Kestral Construction Products Ltd, St. Helens, WA9 4HY

DATAS/7819